## Slide 1: Next Generation Environmental Barrier Coatings
B. A. Pint and K. A. Kane
Corrosion Science & Technology Group Materials Science and Technology Division
Oak Ridge National Laboratory
Oak Ridge, TN 37831
November 6, 2019

## Slide 2: Acknowledgments
Funding from U.S. DOE, Office of Fossil Energy, Turbine Program
  Rich Dennis, Manager; Rin Burke, Project Monitor
  Nuclear Science User Facility: FEI Talos F200X S/TEM
ORNL Team
  J. A. Haynes - TBC procurement
  M. J. Lance - characterization (PSLS, GDOES, Raman)
  K. A. Unocic – TEM (D. Coffey – FIB)
  E. Cakmak – XRD
  G. Garner, M. Howell - oxidation experiments
  T. Lowe - SEM
  T. Jordan, T. Geer – metallography
  E. Lara-Curzio, J. A. Haynes, R. Lowden – input on CMCs
Stony Brook Univ., Center for Thermal Spray Research
  S. Sampath and E. Garcia-Granados

## Slide 3: ORNL project moving from turbine coatings for metals (TBC) to turbine coatings for ceramic matrix composites (EBC)
Superalloys/TBCs
SiC/SiC
CMCs
UHT
CMCs
150oC
~175oC
LEAP aero engine
DOE turbine targets
CMC = Ceramic Matrix Composite, UHT = ultra high temperature
Structural materials temperature capacity
Part 1: Thermal Barrier Coatings
durable
oxidation resistant
low T conductivity
Part 2: Environmental Barrier Coatings
- durable, H2O stable

## Slide 4: Looking for turbine TBC improvements
Focus on thermally-sprayed coatings
  HVOF: high-velocity oxy-fuel
  APS: air plasma spray
  VPS: vacuum plasma spray
  Fabricated at Stony Brook’s CTSR
Project specifics
  Focus on alumina scale “weak link”
  Original goal to push deployment of multi-layer coatings
  Directional solidified 247 superalloys
  PWA286: NiCoCrAlYHfSi bond coatings
Material | Ni | Co | Cr | Al | Y | Hf | Si | Ti | W | Ta | Mo | C | Other (ppmw)
YHfSi Bond Coating | 48.0 | 21.6 | 16.7 | 12.3 | 0.68 | 0.25 | 0.36 | < | 0.01 | < | < | < | 2 S
Y-only Bond Coating | 47.1 | 23 | 16.6 | 12.8 | 0.42 | < | 0.04 | < | 0.02 | < | < | < | 8 S
Alloy 247 | 59.1 | 10.2 | 8.5 | 5.6 | < | 1.32 | 0.06 | 1.0 | 10.0 | 3.2 | 0.6 | 0.2 | 200 Re, 11 S
Superalloy substrate
Dense or DVC YSZ Layer - High KIC
Erosion & CMAS resistant GDZ Layer Dense or DVC architecture
Porous TBC (YSZ or GDZ)
Low conductivity
Low Elastic modulus
Bond coat
ORNL: Environments (higher H2O, CO2, SO2)
CTSR:
Multi-layer top coatings
Al2O3 scale
Optimal bond coating:
Y+Hf+Si
Explored different superalloy substrates

## Slide 5: All TBC testing in simulated exhaust gas: air + 10%H2O
Many studies have shown that water vapor decreases FCT life
1-h cycles:
automated cyclic rig
(10 min cool in lab. air)
20 cycles/day
100-h cycles (base-load):
Tube furnace with endcaps
1 cycle/week
lid
furnace

## Slide 6: Learned many things by changing specimen geometry…
AM 718 “blade”
Coating development not linear with time
2015: 247 rods
Jülich 2014
Cranfield 2013
Not pursued
2018
Superalloy 247 substrates

## Slide 7: APS Flash coatings (Y vs. YHfSi) on alloy 247 disks
Dense YHfSi HVOF layer in each case
Outer APS flash coatings contain internal oxidation generated during APS deposition
More internal oxidation in YHfSi APS layer
  Sprayed same powder size
  Due to higher RE content?
100 µm
Y-only Flash Coating
(0.42 Y)
YSZ
247
HVOF
APS
YHfSi HVOF-only
(0.68 Y, 0.25 Hf, 0.36 Si)
YHfSi Flash Coating
(0.68 Y, 0.25 Hf, 0.36 Si)
HVOF
APS
HVOF
YSZ
247
YSZ
247
Material | Ni | Co | Cr | Al | Y | Hf | Si | Ti | W | Ta | Mo | C | Other (ppmw)
YHfSi Bond Coating | 48.0 | 21.6 | 16.7 | 12.3 | 0.68 | 0.25 | 0.36 | < | 0.01 | < | < | < | 2 S
Y-only Bond Coating | 47.1 | 23 | 16.6 | 12.8 | 0.42 | < | 0.04 | < | 0.02 | < | < | < | 8 S
Alloy 247 | 59.1 | 10.2 | 8.5 | 5.6 | < | 1.32 | 0.06 | 1.0 | 10.0 | 3.2 | 0.6 | 0.2 | 200 Re, 11 S
Notes: Same powder size.

## Slide 8: Y-only flash coating out-performed HVOF by 71%
HVOF as baseline
50 µm APS flash coating
Y only (0.42%Y) vs.
YHfSi (Y+Hf = 0.93%)
5 specimens of each coating
1-h cycles
1100°C
Air+10%H2O
Statistically significant results!
Lance et al. Oxidation of Metals 2019
+12%
+71%

## Slide 9: Why did the Y-only flash coating increase lifetime 71%?
Intermixed alumina-metal layer inhibited crack growth; possibly acted to reduce CTE mismatch in system
Dense HVOF layer was a barrier for substrate attack and provided an Al reservoir for the flash coating (inhibited Ni-rich oxide).
Less reactive element in the Y-only flash coating reduced the rate of Al consumption, thereby increasing lifetime
Flash coating
HVOF coating
Substrate
YSZ

## Slide 10: 2019 Rods: all flash coatings outperformed HVOF and VPS Statistically, did not see additional benefit of Y-only flash
Flash YHfSi Rod (2800 h)
Flash Y-only Rod (2900 h)
epoxy
epoxy
Porous YSZ
Porous YSZ

## Slide 11: Rod characterization: All coatings show similar residual stress in alumina Faster alumina growth on VPS bond coatings with Y+Hf
(a)
(b)
HVOF YHfSi, 2500 h
VPS YHfSi, 1200 h
YSZ
oxide scale
oxide scale
10 µm
YSZ
10 µm
PSLS of rod specimens
Measure same location each time
SEM backscattered electrons
Z-contrast shows Y- & Hf-rich oxides
Oxidation extrapolation
Assuming parabolic kinetics
Similar alumina residual stress
Faster alumina growth on VPS
= faster alumina consumption
Lance et al. Surf. Coat. Tech. in press (presentation at ICMCTF 2019)

## Slide 12: Had to try one more TBC experiment… Lots of questions about flash coating comparison to: 100% APS bond coating and thicker flash coating
5 of each specimen type

## Slide 13: LEAP: 1st Gen. Fiber-reinforced ceramic matrix composites deployed 2nd Gen. to enable ≥65% combined cycle power generation efficiency
Superalloys/TBCs
SiC/SiC
CMCs
UHT
CMCs
150oC
~175oC
LEAP aero engine
DOE Impact: Next generation, ultra high efficiency, utility turbines may require ~1500°C structural materials capability AND 25,000 h lifetime (~10X increase vs. aero applications)
DOE turbine targets
CMC = Ceramic Matrix Composite, UHT = ultra high temperature
Structural materials temperature capacity

## Slide 14
Beyond SiC
Past, Present & Future: ORNL Contributions to CMCs
1960
1970
1980
1990
2000
2010
2020
2030
ORNL: Vapor coating of
ceramic fuel particles
ORNL Developed
forced-flow, thermal-gradient,
Chemical Vapor Infiltration (CVI) process
(1992-2002) DOE Continuous
Fiber Ceramic Composite (CFCC) Program led by ORNL
in close collaboration w/ industry (e.g., GE).
• Advanced CVI
• Interfaces & coatings
• Characterization
• Oxidation testing
SiC/SiC to engine market >25 yr
CFCC
ends
2016
LEAP engine
After CFCC, GE invested
15 yr & ~$1.5B in CMCs
CFCC
begins
CVI : 1980s – 2000’s
Si-free SiC/SiC
Gen-2
UHT
CVI
matrices
New
ceramics
CVD SiC Matrix
Pyrolytic C Interlayer
Ceramic Fiber
ORNL Recent: SiC/SiC
for accident tolerant
nuclear fuels, CVD ZrC
for Space Power.
Gen-1: Si-MI SiC matrices
Malden Mills
CMC liner for
CHP (1999)
-Solar Turbines
-ORNL
-Pratt & Whitney
-BF Goodrich
-Honeywell
-ANL
ORNL future
BAP
arrives
(1994-2001) DOE Advanced Turbine Systems (ATS) Program transferred aero-engine technology to power generation
Thermal barrier coatings
Single crystal superalloys

## Slide 15: Where to get started in 2018 on EBCs?
Parameters
  Coat high-purity CVD SiC (CMCs hard to find)
  First experiments at 1425°C: No Si bond coating
  Coatings made at Stony Brook CTSR
    What parameters to use?
Objectives:
  FY18: Does coating porosity affect performance?
  FY19: What does a lifetime model look like for CMCs in turbine?
    What are failure mechanisms and reaction rates?
      Milestone #1: measure oxidation kinetics at 3 temperatures ±Si bond coating
    What is failure criteria?
      Milestone #2: measure CTE of 2+ EBC components
    Milestone #3: initial estimate of critical temperature for 25,000 hr lifetime
  Difficult to coat CVD SiC without bond coating
  What parameters to use?
  Does coating porosity affect performance?
    Spray distance affects coating porosity: 100 vs. 180 mm
100 mm
Si
Mixed
Ba-Sr-Al-Si-O
SiC

## Slide 16: Exposures to H2O in several rigs at 1300°-1425°C
1-h cycles: automated cyclic rigs
(10 min cool in lab. air)
lid
furnace
Current:
maximum 1300°C
New rig:
>1400°C
1500°C
maximum
1700°C
maximum
Nuclear Severe Accident Test Station

## Slide 17: Start at 1425°C with bare SiC specimens
High temperature furnace:
Gas flow
  ~16 cm/s in steam (slow relative to turbine)
  ~6 cm/s in air (500 cc/min)
Expected mass loss due to Si(OH)4 evaporation
Similar mass loss for both CVD SiC and Hexoloy
Improved holder made for exposures in TGA at 1425°C

## Slide 18
Scale
Substrate
TEM: Thicker scale formed in steam and finer porosity
1µm
Voids/porosity
Crack parallel to the matrix/scale interface
Note: different magnification
100 h, dry air
100 h, steam
1.8±0.04 µm
4.9±0.5 µm
TEM annular
dark field

## Slide 19: 1425°C exposures: similar mass change for 4 coated SiC
5 x 20-h cycles in 100% H2O
Gas flow rate ~16 cm/s 100% steam
Only one side of CVD SiC specimen coated with sprayed Yb2Si2O7
Similar mass loss for all 4 specimens
Comparisons to isothermal uncoated CVD SiC specimens
  No thermal cycling on uncoated SiC

## Slide 20: Yb2Si2O7 coated CVD SiC: D porosity by spray distance 100 mm (15.4±1.8%) vs. 180 mm (13.1±3.4%) 2nd parameter: 1300°C pre-anneal to crystalize Yb2Si2O7
After 100h, 1425°C, 100% steam
Light microscopy
Poor EBC adhesion without anneal
With anneal:
Not much better

## Slide 21: Sections showed reaction products under EBC all were similar in thickness to uncoated SiC: no EBC effect
After 100h, 1425°C, 100% steam
Thicker oxide than formed on bare SiC

## Slide 22: Issue with Al contamination at 1425°C in steam Reaction of Al2O3 specimen holder and reaction tube
Annealed 180 mm spray distance after 100h, 1425°C, 100% steam
SEM/EDS maps

## Slide 23: All future EBC specimens will be annealed 1300°C: EBCs without anneal failed within 20 1-h cycles
All specimens cut first
100 mm spray distance
180 mm spray distance
No anneal prior to cycling
Annealed 4h/1300°C
All images after 20, 1-h cycles
in air+90%H2O

## Slide 24: With annealing, coatings survived 500 1-h cycles in air+90%H2O
SiC
YbDS
20µm
Silica

## Slide 25: With & without Si bond coating, EBC was effective at 1300°C in reducing SiO2 thickness after 500 x 1-h cycles
Reduced silica thickness: EBC effective
Measured SiO2 thickness
Part of FY19 Milestone #1

## Slide 26: Initial CTE measurements
Thermal (cooling) stress: sox = - Eox•ΔT•(aalloy - aoxide)/(1-u)
Strain Energy: W = f(doxide) : dspall = f(ΔT•Δa)-2 (critical scale thickness for spallation)
SiC Δa ~ 4 at 1200°C
SiO2 and SiC specimens:
Part of FY19 Milestone #2
Making Yb2Si2O7 and Yb2SiO5 samples

## Slide 27: Initial CTE measurements
Thermal (cooling) stress: sox = - Eox•ΔT•(aalloy - aoxide)/(1-u)
Strain Energy: W = f(doxide) : dspall = f(ΔT•Δa)-2 (critical scale thickness for spallation)
SiC Δa ~ 4 at 1200°C
If NiAl: Da ~5.8
d=10 µm at 1200°C
Then SiC: Da ~4
d=15 µm at 1400°C
& Si: Da ~3.4
d=21 µm at 1400°C

## Slide 28: Annealing: more affect on EBC performance than porosity
1st batch of EBC specimens evaluated with two porosity levels
  Yb2Si2O7 on CVD SiC with and without annealing
  No coatings were protective at 1425°C
  Better 1300°C adhesion after initial 4h/1300°C anneal
Experimental procedure being evaluated in high T steam
  Issue with alumina contamination
Assessing the next generation of EBC’s for power generation
  Is 25,000 h lifetime viable?
  Collecting more data at 1250°-1350°C
  With and without Si bond coating
  Collecting CTE data to model failure

## Slide 29: Backup slides

## Slide 30: 1300°C: EBCs without anneal failed within 20 1-h cycles
All specimens cut first
100 mm spray distance
180 mm spray distance
No anneal prior to cycling
Annealed 4h/1300°C
All images after 20, 1-h cycles in air+90%H2O

## Slide 31: Ran two more flash-coated specimens to 300 cycles: YHfSi flash coating: Al was more depleted in HVOF layer
YHfSi: more oxide = more Al consumed = shorter life
Al wt.%
100 µm
Y-only Bi-layer
YHfSi Bi-layer
β-NiAl
SEM images
Aluminum EDS Concentration Maps
After 300 1-h cycles at 1100°C in air+10%H2O
Al2O3
Al2O3
100 µm
Notes: These are two NOT FAILED sections.
We didn’t think there would be a large difference.
The finer splat size in the YHfSi outer flash coating compared to the Y-only flash coating in the as sprayed condition leads to more oxidation and more rapid Al depletion and earlier lifetimes. Therefore, the benefits of having an APS flash coat layer are partially offset for the YHfSi coating by too much internal oxidation.

## Slide 32: Failure microscopy: HVOF and flash-coat differences
HVOF-only: smoother interface, more uniform oxide
Much more oxide formed with flash coatings
Underlying HVOF layer inhibited superalloy oxidation
Intermixed metal/oxide layer: inhibited interface crack growth
Intermixed metal-oxide layer: did it create a graded interface & reduce CTE mismatch?
Y-only Flash, 1080 cycles
YHfSi Flash, 760 cycles
YHfSi HVOF-only, 620 cycles
100 µm
100 µm
100 µm
YSZ
Notes: which may explain its earlier failure as the interfacial crack can easily extend across the entire specimen without deflecting
We grade to Al2O3 not YSZ.
Segue: It is hard to make comparisons after failure because they each lasted different cycle times, so we took another samples and cycled to 100 and 300 cycles.

## Slide 33: Starting bond coating conditions
HVOF-only coating slightly thicker (but had lowest life)
Roughness did increase with flash coating
Measured fractal dimension (Df) as described by Nowak et al. (Jülich)
  Fairly small differences measured to explain 12% and 71% increase in lifetime
Starting Bond Coating Thicknesses
Starting Roughness and Fractal Dimension
Notes: Roughness was significantly lower than reported for other bond coatings.
Just state what the thicknesses were; don’t apologize.
Couldn’t test the effect of this parameter like Nowak did.
We are working on the fractal dimension like Nowak.
Summit density

## Slide 34: In-situ coating characterization using PLPS through YSZ
5 cycles at 1100 °C
100 cycles at 1100 °C
100 cycles at 1150 °C
300 cycles at 1100 °C
a
d
c
b
200 µm
Compressive
Stress (GPa)
1-h cycles in ”wet” air (10%H2O)
PLPS: photo-stimulated luminescence piezospectroscopy

## Slide 35: Is roughness really the “flash” coating advantage? Stony Brook: could not correlate roughness with lifetime
1100°C (2102°F)
24-h cycles
Laboratory air
3 specimens/group
15 profilometry measurements to determine roughness

## Slide 36: PLPS results: very weak signal through 300µm top coating
Similar residual stress in alumina scale on both bond coatings
Higher residual stress in flat disk specimen compared to rods

## Slide 37: 2nd Iteration Model of 900°C (1650°F) coating performance
Cr content (%)
Distance (µm)
Molar Phase Fraction
Concentration (%)
Experiments (isothermal)
Model predictions at 900°C (DICTRA)
Results by K. Kane (VCU) and R. Pillai (ORNL)