## Slide 1
Minking Chyu, Albert To University of Pittsburgh
Bruce S. Kang West Virginia University
Integrated Transpiration & Lattice Cooling Systems Developed by Additive Engineering with Oxide Dispersed Strengthened (ODS) Alloys

## Slide 2: University Turbine Systems Research
Outlines
Background, Challenges, Objectives, Benefits of Technology, Research Task Plans
Additive Manufacturing Processes
ODS Powder Development
Heat Transfer Results: Transpiration Cooling
Heat Transfer Results: Lattice Cooling
Summary
Notes: Presentation outline:
A brief introduction to the challenges in turbine blades, which are related to our project.

## Slide 3
Technical Background: Need for Turbine Cooling
Turbine Inlet Temperature continues to rise
“One key will be the marriage of design and manufacturing to bring about the concurrent use of engineered micro cooling or transpiration, with the ability of additive manufacturing. If successful, this combination could see a further 50% reduction in coolant usage for turbines”
Bunker RS. Evolution of Turbine Cooling. ASME. Turbo Expo: Power for Land, Sea, and Air, Volume 1: Aircraft Engine; Fans and Blowers; Marine; Honors and Awards ():V001T51A001. doi:10.1115/GT2017-63205.
Notes: This viewgraph on left summarized the projected turbine inlet temperature of advanced gas turbine engines that continue to increase, which demands higher cooling load to combat the aerothermal challenges.
The right view graph is from Bunker 2017. The “heat load parameter” is basically a non-dimensional mass flow rate of the coolant. The figure illustrated the progressing of cooling technologies over the past few decades. Overall cooling effectiveness has been increased from 0.1 at the beginning to 0.7 today, which includes the contribution of convection cooling, film cooling, and TBC. Meantime, the coolant amount instantly decrease with the progress with time, to enhance the turbine cycle efficiency.
Bunker pointed out that “one key avenue for turbine airfoil cooling might be “bringing about micro cooling or transpiration cooling with the ability of additive manufacturing”. By introducing complex geometry to achieve near wall or transpiration cooling, the coolant usage might be further reduced for 50%.
Typical failure of turbine blades included hot corrosion, thermal fatigue and thermal creep. All related to the high temperature condition the airfoils suffers from.
As a consequence, novel cooling technology and new material are urgently in need.

## Slide 4
Technical Background
Siw, S.C., Chyu, M.K., Karaivanov, V.G., Slaughter, W.S., and Alvin, M.A., 2009, “Influence of Internal Coolinjg Configuration on Metal Temperature Distributions of Future Coal-Fuel Based Turbine Airfoils,” Turbo Expo 2009, GT2009-59829.
Bunker, R.S., 2013, “Gas Turbine Cooling: Moving from Macro to Micro Cooling,” Turbo Expo 2013, GT2013-94277
Near surface ‘skin cooling’ or ‘double-wall’ internal cooling arrangement leads to a significant reduction of metal surface temperature, which can be in the order of 100 degrees, compared to conventional serpentine cooling designs
Notes: This viewgraph on left summarized the projected turbine inlet temperature of advanced gas turbine engines that continue to increase, which demands higher cooling load to combat the aerothermal challenges.
The right view graph is from Bunker 2017. The “heat load parameter” is basically a non-dimensional mass flow rate of the coolant. The figure illustrated the progressing of cooling technologies over the past few decades. Overall cooling effectiveness has been increased from 0.1 at the beginning to 0.7 today, which includes the contribution of convection cooling, film cooling, and TBC. Meantime, the coolant amount instantly decrease with the progress with time, to enhance the turbine cycle efficiency.
Bunker pointed out that “one key avenue for turbine airfoil cooling might be “bringing about micro cooling or transpiration cooling with the ability of additive manufacturing”. By introducing complex geometry to achieve near wall or transpiration cooling, the coolant usage might be further reduced for 50%.
Typical failure of turbine blades included hot corrosion, thermal fatigue and thermal creep. All related to the high temperature condition the airfoils suffers from.
As a consequence, novel cooling technology and new material are urgently in need.

## Slide 5: Proposed Technologies
Substrate (Superalloy)
ODS Structural Layer
αAl2O3 / NiO
Internal Cooling Passage
ODS Layer Cooling Passage
Near Surface Embedded Cooling Channel (NSECC )
Integrated Transpiration and Lattice Cooling Systems
Transpiration Cooling
Internal Cooling
Hollow Lattice
ODS with AM
Both internal and external protection.
Oxidation Resistance
Realized with additive manufacturing
ODS
Enhanced oxidation resistance and high temperature strength
Advanced Additive Manufacturing
Intricate Heat Transfer Enhancement Features
Enhanced Heat Removal
NSECC: high internal heat transfer and higher coolant flow near hot end wall.
Lattice and transpiration combined conjugate cooling: ~2x of state-of-the-art film cooling.
Novel ODS Surface Coating
Ultra-High Temperature (1200C) Strength: thinner outer wall for better cooling
Oxidation Resistance
Higher turbine inlet temperatures
Notes: Such a marriage between material and manufacturing is the prime focus of our two UTSR research. The novel ODS material being developed has been proven to have extremely high oxidation resistance and high temperature strength (1200 C). This high strength makes it difficult for conventional machining to be used to form parts from ODS. However, we showed that AM is a viable approach to consolidate ODS powder into desired part form or coating.
The first project demonstrated the use of DED for deposition of ODS on superalloy substrate. This allowed to push the cooling channels closer to the hot side end wall and also in thinner end wall owing to the high temperature strength of the ODS.
The second project focuses on taking this approach further by fabricating a novel integrated transpiration and lattice cooling structure out of ODS. Such a geometry takes the advantage of AM and ODS and is capable of providing external and internal thermal protection in addition to being less susceptible to oxidation.

## Slide 6
Lab-Scale Heat Transfer Characterization
CFD modeling & steady state and scaled TLC testing
Mini/micro scale cellular units
ODS Powder Fabrication and Characterization
MCB/BM for powders fabrication
Characterization
Thermal Cyclic Testing
In-situ non-destructive micro indentation facility
Thermal Cyclic Tests, Micro-hardness
Combustor
Aerothermal Test Section
Process Optimization to Fabricate ODS Transpiration and Lattice Structures
DMLS, BJT printing parameters
Posting printing characterization
OM, SEM
High Temperature Heat Transfer Characterization
High Temperature, Pressurized Testing (NETL)
Cooling Geometry Design
Wall jets, Transpiration and Lattice Geometry development and optimization
Project Work Breakdown Structure
Goal: Enhanced Oxidation Resistance and Thermal Protection of Turbine Blades
Notes: Main advantages:
Provide protection from oxidation and ultra high temperature strength
provide cooling efficiency more than 0.6.
Complex ODS lattice structure, - ultra high temperature strength, coupled with high oxidation resistance.
Broadly speaking, the Projects have following 6 sub-tasks
– U Pitt is responsible of exploring different configurations that can be considered as wall jet geometries, and Integrated Transpiration and Lattice Cooling Systems. Siemens will also provide suggestions and guidance on this part.
– U Pitt will develop optimal AM process for ODS lattice structure in the ANSYS Additive Manufacturing Research Lab. Siemens has rich experience on AM turbine components and we will exchange knowledge during this phase.
- U Pitt and NETL will conduct high temperature heat transfer experiments on the finalized ODS lattice structures
– WVU will further improve the production process and continuously produce adequate powder for the AM process. The time cost will be further reduced.
- WVU will exam the oxidation characteristics of ODS lattice structures under cyclic high temperature conditions to prove anti-oxidation properties of ODS.

## Slide 7: University Turbine Systems Research
Outlines
Background, Challenges, Objectives, Benefits of Technology, Research Task Plans
Additive Manufacturing Processes
ODS Powder Development
Heat Transfer Results: Transpiration Cooling
Heat Transfer Results: Lattice Cooling
Summary
Notes: Presentation outline:
A brief introduction to the challenges in turbine blades, which are related to our project.

## Slide 8
As metallic additive manufacturing technologies advance significantly over the recent past, complex metal products, such as turbine components, can be manufactured by this innovative technology.
Bind Jetting
(EXOne)
Powder Bed Fusion (EOS)
Direct Energy Deposition (LENS)
Pros: geometry free
cons: high porosity
Pros: complex geometry
cons: single material
Pros: multiple materials
cons: no overhangs or unsupported structure
AM Processes Utilized
Notes: Binder Jetting: ExOne. Adhesive binder to form the built product, then heat treatment to burn away the binder and create sintering effects to form the product. The advantage is that the energy to produce the build is low and without laser melting; but the product with too high porosity, such as hipping process.
EOS is laser melt powder bed process and is very popular in aero and energy sectors. EOS provides recipe of process for a number of materials
LENS is a direct laser-melt particle deposit technology. This is a popular method for part repairing and using the method to develop new material or composite of new material characteristics. The limit is that this is a “free-form” technology, not a “powder bed” technology, so the part-building is processed without lateral support; hence it is difficult to bulid bridges and hangovers.
Powder Bed Direct Metal Laser Sintering: EOS
a production machine for complex geometries
Direct Energy Deposition: LENS
for multiple material or coating/combining materials
do not allow overhangs or unsupported structures

## Slide 9: University Turbine Systems Research
Outlines
Background, Challenges, Objectives, Benefits of Technology, Research Task Plans
Additive Manufacturing Processes
ODS Powder Development
Heat Transfer Results: Transpiration Cooling
Heat Transfer Results: Lattice Cooling
Summary
Notes: Presentation outline:
A brief introduction to the challenges in turbine blades, which are related to our project.

## Slide 10
Pros and Cons of Gas Atomization (GA)
for AM Metal Powder
Pros:
Atomization processes are capable of producing high quality metal powders, such as aluminum, brass, iron, stainless steel, titanium and superalloys with uniform particle distribution and spherical shape.
Current standard fabrication method to produce metal powders for metal AM.
Cons:
ODS powder fabrication using GA becomes problematic due to high melting temperature of yttrium oxide (Y2O3, 2425°C) compared to iron (Fe, 1538 °C), nickel (Ni, 1668 °C), chromium (Cr, 1907 °C) and aluminum (Al, 660 °C), thus, uniform dispersion of Y2O3 is problematic for production of ODS powders.
Post alternations of atomized powder (i.e. ball milling) must be done to produce ODS powder.

## Slide 11: Ni- and Fe-based ODS powder development for Additive Manufacturing of gas turbine component with better high temperature (up to 1200 oC) oxidation/corrosion resistance and material strength (i.e. creep and fatigue)
(i) (to produce) ODS powder for AM with lower manufacturing cost and better yttria dispersion using a combined Hosokawa mechano chemical bonding (MCB) and ball milling (BM) process:
(a) MCB + BM
(b) MCB only
(ii) AM processing optimization
(iii) (to achieve) a durable α-Al2O3 oxide layer (via external oxidation) with strong adhesion to substrate for better oxidation and corrosion resistance (e.g. molten chloride)

## Slide 12
SEM micrographs of MCB processed ODS powder sample
(a). As-processed from MCB; (b) close view of (a)
Cr (7.5~10 µm) | Al (4.5 ~ 7 µm) | Y2O3 < 50nm | W (~1 µm) | Ni (4 ~ 8 µm)
20 | 5 | 1.5 | 3 | 70.5
Mechano-Chemical Bonding (MCB) Technique
*Challenge: uniform dispersion of nano-sized Y2O3 through out the matrix
Hosokawa MCB machine
Mixing time: 1hour
Y2O3 is uniformly coated
on master particles
Ball milling time: 40 hours
Forming alloyed ODS powder
Notes: Benefits of ODS – Y2O3 – high temp creep alloy
How to uniformly dispersed Y2O3 onto the alloy?
Y2O3 gave high temperature resistance
Challenge in ODS community is to coat Y2O3 on the master particle

## Slide 13
ODS Powder Characterization
TEM BF image (a) shows a layer of Y2O3 thin film with thickness about 25nm around the edge of particle. The film thickness is relatively homogeneous.
HREM image (b) shows the fine structure of the thin film. Most area of the film is amorphous and the corresponding FFT (Fast Fourier Transform) image show the diffusive feature.
There is crystal structure within film as FFT indicated. The embedded FFT shows the spots and image shows the orientation fringe. The growth of film may involve crystallization of Y2O3.
Notes: Each host/master particle – evidently clear that coated with Y2O3.
BF: bright field mode of the TEM (to show Y2O3)
The following areas appear with dark contrast in BF mode:
thick areas,
areas in which heavy atoms are enriched,
crystalline areas
HREM: High-resolution transmission electron microscopy

## Slide 14: XRD of ODS Powders MCB only, MCB + Ball Mill for 20 hours, and MCB + Ball Mill for 40 hours
Ni3Al-
NiAl-
Cr-
Ni-
W-
Al-
C5 depicts MCB plus ball milling process for 20 hours at 400 rpm, with a BPR of 15:1.
C6 depicts MCB plus ball milling process for 40 hours at 400 rpm, with a BPR of 15:1.

## Slide 15
ODS Powder processed by MCB+BM
Ni-20Cr-5Al-3W-1.5Y2O3 in Weight.%

## Slide 16
MCB only

## Slide 17
Mechano-Chemical Bonding (MCB)
XRD, ODS powders (MCB only, M6)
XRD, AM sample (M6 ODS powder)
MCB only, M6 ODS powder, 5000 rpm 11 hours

## Slide 18
1
Powder
Printing Parameters
Heat
Treatment
MCB 4000rpm 1h, +BM 400rpm 40h
250W,5mm/s,
0°+90°
2
250W,10mm/s,
0°+90°
3
MCB only, 5000rpm 11h, acid+sieved
250W,10mm/s,
0°+90°
100W,
10mm/s
MCB only, 5000rpm 11h, acid+sieved
250W,10mm/s,
0°+90°
200W,
10mm/s
MCB 4000rpm 1h, +BM 400rpm 40h
7
MCB 4000rpm 1h, +BM 400rpm 40h
250W,15mm/s,
0°+90°
N/A
N/A
N/A
4
MCB 4000rpm 1h, +BM 400rpm 40h
250W,10mm/s,
0°+90°
100W,
10mm/s
5
MCB 4000rpm 1h, +BM 400rpm 40h
250W,10mm/s,
0°+90°
200W,
10mm/s
6
ODS Coatings by LENS
10mm x 10mm x 0.5~1mm
Flowability of MCB only powder improved significantly
Surface becomes smoother after 200W laser surface heat treatment.
Scan Speed
Heat Treatment
Notes: In general, the MCB + BM powders show good flowability for AM systems, which can provide stable flow rate in LENS system.

## Slide 19
2
2b
1a
1
1b
2a
8
6
7
2
Powder
Printing Parameters
Heat
Treatment
MCB 4000rpm 1h, +BM 400rpm 40h
250W,10mm/s,
0°+90°
2a
250W,10mm/s,
0°+90°
2b
MCB only, 5000rpm 11h, acid+sieved
250W,10mm/s,
0°+90°
100W,
10mm/s
MCB only, 5000rpm 11h, acid+sieved
250W,10mm/s,
0°+90°
200W,
10mm/s
MCB 4000rpm 1h, +BM 400rpm 40h
MCB 4000rpm 1h, +BM 400rpm 40h
250W,10mm/s,
0°+90°
N/A
100W,
10mm/s
200W,
10mm/s
1b
MCB 4000rpm 1h, +BM 400rpm 40h
250W,5mm/s,
0°+90°
200W,
10mm/s
8
MCB 4000rpm 1h, +BM 400rpm 40h
250W,10mm/s,
0°+90°
N/A
1
MCB 4000rpm 1h, +BM 400rpm 40h
250W,5mm/s,
0°+90°
N/A
1a
MCB 4000rpm 1h, +BM 400rpm 40h
250W,5mm/s,
0°+90°
100W,
10mm/s
7
6
(MCB only) ODS Coatings by LENS

## Slide 20: Oxidation Weight Gain
Schematic of the cyclic thermal exposure apparatus setup (WVU)
** Each cycle consists of moving test sample to the furnace within 15 minute and kept at 1100 oC for 45 minutes and moved out within 15 minutes, kept for 45 minute at room temperature.
length
width

## Slide 21
[1] Wright, I.G., Pint, B.A. & Tortorelli, P.F. Oxidation of Metals (2001) 55: 333. https://doi.org/10.1023/A:1010316428752
[2] Brady, M.P., Muralidharan, G., Yamamoto, Y. et al. Oxid Met (2017) 87: 1. https://doi.org/10.1007/s11085-016-9667-3
Pitt-WVU ODS: Ni-20Cr-5Al-3W-1.5Y2O3(Thermal cyclic Test at 1100 degree C)
APM FeCrAl: Fe-20.42Cr-5.54Al-0.08Mn-0.03Ti-0.23Si-0.03C( cyclic-oxidation tests,1100 degree C)
ODS Fe3Al: Fe–28Al–2Cr–0.5Y2O3( cyclic-oxidation tests,1100 degree C)
Fe-35Ni-25Cr-4Al+Ti,C/Fe-35Ni-25Cr-4Al+Nb,C/Fe-25Ni-15Cr-4Al( Mass change at 1100 degree C in air with 10% H2O vs. time (100 h cycles)
Chart: Oxidation Weight Gain
| 0 | 40 | 80 | 120 | 160 | 200 | 240 | 280 | 320 | 360 | 400 | 480 | 560 | 640 | 800 | 1000 | 1200 | 1400 | 1600 | 1800 | 1860 | 1920 | 1980 | 2040 | 2100 | 2160 | 2220 | 2280 | 2400 | 2520 | 2580 | 2640 | 2700 | 2760 | 2820 | 2940 | 3000 | 3060 | 3120 | 3180 | 3240 | 3300 | 3345 | 3405 | 3445 | 3485 | 3520 | 3560 | 3600 | 3640 | 3720 | 3760
Pitt-WVU ODS | 1.5489 | 1.8808 | 1.3276 | 2.3234 | 0 | 0.44254 | 0.22127 | 0.77445 | 0.22127 | 0.55318 | 2.3234 | 1.1064 | 1.3276 | 1.4383 | 1.4383 | 1.4383 | 1.4383 | 0.22127 | 1.9915 | 1.8808 | 1.8808 | 1.9915 | 1.8808 | 1.8808 | 1.8808 | 1.8808 | 1.9915 | 2.6553 | 2.5446 | 2.6553 | 2.6553 | 2.6553 | 2.434 | 2.6553 | 2.6553 | 2.5446 | 2.5446 | 2.5446 | 2.6553 | 2.6553 | 2.6553 | 2.8765 | 2.6553 | 2.6553 | 2.9872 | 2.9872 | 2.8765 | 3.0978 | 2.8765 | 2.8765 | 3.2084
APM FeCrAl | 0 | 0.49254 | 0.856 | 1.5661 | 1.055 | 1.7296 | 1.2187 | 1.3356 | 1.4994 | 1.7324 | 1.9076 | 2.1876 | 2.3045 | 2.4676 | 2.5713 | 2.6993 | 2.8276 | 2.9439 | 3.0133 | 3.1882 | 3.2226 | 3.2683 | 3.3379 | 3.4896 | 3.5589
ODS Fe3Al | 0 | 0.29319 | 0.65659 | 0.77365 | 1.283 | 1.0543 | 1.1946 | 1.2647 | 1.3582 | 1.5218 | 1.6619 | 1.8487 | 2.0941 | 2.2221 | 2.3738 | 2.5955 | 2.642 | 2.7587
Fe-35Ni-25Cr-4Al+Ti,C | 0 | 1.0991 | 1.025 | 1.3222 | 1.4335 | 1.5994 | 1.2952 | 1.1719 | 0.79542 | 0
Fe-35Ni-25Cr-4Al+Nb,C | 0 | 0.50305 | 0.61427 | 0.67181 | 0.80116 | 0.80427 | 0.93678 | 1.0667 | 1.1268 | 1.0423
Fe-25Ni-15Cr-4Al | 0 | -3.6898 | -4.9157 | -5.3464 | -6.0303 | -6.2619 | -6.494 | -6.8825 | -6.9337
Weight Gain Comparison (ODS sample 1)

## Slide 22: Microstructure Stability Analyses of AM-processed ODS using LENS
Stability of oxide layer
Stability of interface
Stability of substrate
Stability of ODS coating

## Slide 23: 200W- MCB+BM ODS– AM Printed
Nano-sized ’phase
850nm
ODS Coating
Nano-sized ’phase preserved at ODS coating.

## Slide 24: 200W- MCB+BM ODS – 2200 Cycles
750nm
Nano-sized ’phase
Nano-sized ’phase preserved at ODS coating after 2200 cycles
ODS Coating

## Slide 25: 200W ODS – 2200 Cycles
30um
Aluminum Oxide Scale
Stable 10 – 15 um of uniform stable aluminum oxide scale
Oxide Scale

## Slide 26
Isothermal Test for Full ODS Channel
10 µm
10 µm
100h
200h
10 µm
400h
1200C
1900h
10 µm
800h
1200h
10 µm
10 µm
1600h
10 µm
700h
10 µm
1900h
Oxide layer stables after 100h during Isothermal test.

## Slide 27
Zone : Mainly Al2O3
1
Total thickness of oxide layer is around 10-15 µm, and the Al2O3 dominated layer thickness is 5-10 µm.
1600h
1700h
1
Al
Ni
Cr
O
Thickness (µm)
Weight
Percentage
(%)
1700h
1
Thickness (µm)
1900h
1900h
Stable Alumina in Oxide Layer

## Slide 28: ODS coating stress/strain curve

## Slide 29: University Turbine Systems Research
Outlines
Background, Challenges, Objectives, Benefits of Technology, Research Task Plans
Additive Manufacturing Processes
ODS Powder Development
Heat Transfer Results: Transpiration Cooling
Heat Transfer Results: Lattice Cooling
Summary
Notes: Presentation outline:
A brief introduction to the challenges in turbine blades, which are related to our project.

## Slide 30: Introduction: Transpiration Cooling
Coolant
Mainstream
Turbulence
Mixing Area
Mainstream
Conventional Film Cooling
Transpiration Cooling
High Anti-oxidation Resistance
High Temperature Mechanical Strength
Comparable Strength with Casting
Complexity and Design Freedom
Fast and Low-cost Fabrication for Intricate Features
“Lift-off” of the film due to jet momentum at the outlet
Film gradually spread diffused downstream by flow mixing
ODS
AM
Uniform coolant film coverage
Enhanced heat removal ability due to higher inner-wall heat transfer
Concept: The coolant was forced through a porous wall or multiple micro-cooling channels to form an insulating layer of coolant film between the outer wall surface and hot stream.
Challenges
Oxidation due to Vortex Mixing with Hot Gas
Mechanical Strength Concern with Porous Media
Manufacturing Difficulties
Notes: Now we are working on applying transpiration cooling designs into turbine blade. In general, the transpiration cooling will provide better film coverage and enhance the heat removal ability due to higher inter-media heat transfer compared to conventional film cooling. However, the manufacturing difficulties, mechanical strength concerns and possible oxidation due to vortex mixing with hot gas. As shown in this slides, the development of AM significantly alleviated the manufacturing difficulties for such delicate features. Now the parts made by AM has comparable or even slightly higher mechanical strength than those of cast. In addition, the inherently remarkable mechanical strength and anti-oxidation properties of ODS alloy at high temperature makes it a perfect candidate for turbine airfoil.

## Slide 31
Transpiration & Film Cooling Test Structures
(A) Round
Holes with Pitch of 3D
(RH-3D)
(C) Spheres
Packing
(SP)
(D) Wire Mesh
(WM)
(E) Blood Vessel Shaped
(BV)
(B) Round Holes with Pitch of 2D
(RH-2D)
F
(F) Laidback Film Cooling
(FC)
D=1mm
Design Parameters:
Material: In718
Test Plate Size (mm) : L30×W12×T3.2
Cooling effective area: L20 ×W12
0
;
Injection Ratio:
Notes: As for transpiration part, first we experimentally investigated different structures as shown in this picture and compared to laidback shaped holes film cooling. The structure designs include round holes with pitch of 3D and 2D, sphere packing design which originated from the powder compaction sintering, wire matrix design which comes from woven wire matrix and blood vessel shaped micro-channels design. To fairly compare the cooling performance, only the part of the plate is porous for transpiration cooling coupons to make sure the coolant covered area is the same as the downstream area of the film cooling holes.

## Slide 32
F=1.2% and 2.4%, other 4 transpiration structures > FC ≈ RH-3D
F=3.6%, all 5 transpiration structures > FC
BV and SP are better than others
BV has the highest average cooling effectiveness
adiabatic wall temperature
: wall temperature
TC :coolant temperature
Results – Local Cooling Effectiveness
Notes: This slide shows the heat transfer test results. The figure on the left hand side shows the cooling effectiveness distributions of the effective area.
Based on the results we can see almost all the transpiration cooling structures have higher cooling effectiveness than film cooling except for the RH-3D case at the lowest injection ratio. One possible reason is the cooling passages are not dense enough to provide full film coverage of the hot surface.
At higher injection ratio, all transpiration cooling structures have better performance than film cooling.
Among the transpiration cooling structures the performance of the blood vessel shaped micro-channels seems the best

## Slide 33
AM made specimen
=0%
=3.03%
= 9.52 %
=5.74%
=23.37%
=15.48%
=9.96%
=12.8%
All tensile bars made by AM have much higher ultimate tensile strength than the one made by traditional In718 powder sintering(1250C, 6h).
Tensile Test Results
sintered
porous
Porosity
Notes: This slide the tensile test for the printed coupons(extended work, not included in the paper). The gauge parts of the tensile bars are using the same design of the transpiration cooling and film cooling structures for heat transfer test. One porous media made by conventional powder sintering process has also been tested in this test. The strain-stress curve showed that all tensile bars made by AM have much higher ultimate tensile strength(at least 2-3 times) than the one made by traditional In718 powder sintering(1250C, 6h).

## Slide 34: Effect of Hole Configurations
Cooling Effectiveness of Different Hole Configurations
θ
Porosity: 1) inline and staggered P=nD: ϕ(n) ~ 1/n2
2) inclined: ϕ(n, θ) ~ 1/n2cosθ
Notes: This slide shows the effect of hole configurations, two major findings are:
Smaller pore size increases the ratio of the internal air-metal interface area to the volume(compactness), thus the cooling effectiveness is enhanced for the same hole pitch
Staggered hole pattern or inclined cooling channel towards downstream also increase the cooling effectiveness by providing better coolant film coverage and reduce the lift-off of the film.
Porosity: 1) inline and staggered P=nD: ϕ(n) ~ 1/n2
2) inclind: ϕ(n, θ) ~ 1/n2cosθ
Internal Surface: 1) inline and staggered P=nD : Ai ~ 1/ n2D
2) inclind: Ai ~ 1/ n2Dcosθ

## Slide 35: University Turbine Systems Research
Outlines
Background, Challenges, Objectives, Benefits of Technology, Research Task Plans
Additive Manufacturing Processes
ODS Powder Development
Heat Transfer Results: Transpiration Cooling
Heat Transfer Results: Lattice Cooling
Summary
Notes: Presentation outline:
A brief introduction to the challenges in turbine blades, which are related to our project.

## Slide 36
Challenges:
AM process parameters for ODS
Controlling dimension change and deformation
Identify minimum limitation of pore diameters
Internal Cooling with Macro Scale Lattice (Phase 1)
Transpiration Cooling with Micro Scale Lattice (Phase 2)
Combined Internal and External Cooling with Multi-scale Lattice (Phase 3)
Approaches to Fabricate ODS Lattice Structures
Coupon with solid lattice and porous channel wall
Notes: There are three phases to explore the ODS lattice structure:
Phase 1 will focus on the internal cooling usage of lattice structures. The main effort is to figure out the AM process parameters and printable capable dimensions.
Phase 2 will consider the application in transpiration cooling and the lattice will have smaller scales. The main challenge is the printing quality of the pores.
Phase 3 will integrate the geometry from the previous two phases and develop a combined internal and external cooling approach. This is targeted at high cooling efficiency and robust anti-blockage property.
The image on the right bottom corner shows an exploratory intermediate step between phase 1 and phase 2. The coupon has an internal solid lattice network and an external porous wall with transpiration holes (0.3 mm, 2D pitch). The coolant is introduced from the left in the internal channel. This coolant then flows over the lattice and parallel to the channel wall to provide internal cooling. In addition, the spent coolant also bleeds through the transpiration holes to form the external protective film coverage.

## Slide 37
Kagome (corner sharing triangles)
Body centered (BC)
Octahedral (Octa)
Parameters
Ligament diameter: d
Unit cell base: a
Unit cell height: h
Porosity: p
Total surface area: Asurf
Footprint area: Afp
Orientation with flow:
Face centered (FC)
Top view
Front View
Perspective
Top view
Front View
Perspective
Top view
Front View
Perspective
Overview of unit cells under investigation:
Internal Cooling with Macro Scale Lattice (Phase 1)
Top view
Front View
Perspective
a
h
= 0
= 45
Notes: This slide summarized different type of unit cells and preliminary heat transfer results of two Kagome lattices.
Lattices in a cubic unit can have different topologies by changing the connection between the vertices. Meantime, the diameter of each connection bar can vary to form different density or opening.
Besides the cubic lattices, there are still numerous bionic or irregular shaped lattices to explore, e.g blood vessel lattices
The tetrahedral lattice is relatively more used in making components with lighter weight but desired stiffness. Tetrahedral name refers to the “tetrahedron” formed by the top as well as the bottom ligaments of the unit cell.
The cubic lattice unit cells are derived from the prevalent molecular lattice unit cells in crystals. Body centered and face centered names are derived from the location of the node formed from intersection of the ligaments. The octahedral unit cell is a slight modification of the facecentered, wherein, an additional 4 sided pyramid like structure has been introduced on both top and bottom half of the unit.
Some of the ky parameters are depicted which include the ligament diameter, unit cell dimensions, surface area and porosity. In addition, the angle at which the flow is incident with respect to the upstream face forms another parameter.

## Slide 38: Lattice Geometries
BC 0
FC
OCTA0
Pin HD2 SD2.5
Kagome
BC 45
FC 45
OCTA45
True scale unit cell
a = 4 mm
h = 2.54 mm
θ = 0 and 45 degrees
D = 0.75 mm
Scaled up (5x)
a = 20 mm
h = 12.7 mm
D = 3.75 mm
Thermally inactive lattices
Fabricated using SLA
Nylon pin fins
Transient liquid crystal technique for HT studies

## Slide 39: Measured Local HTC at Re ~15100
BC
FC
OCTA
Kagome
0 degree
45 degree
Top Plate
Bottom Plate
Pin Fins
HD2 SD2.5
Notes: HTC distribution varied among the cases.
  BC: near channel center
  FC: near vertices, around the junction of rods for 0 degree; more evident for 45 degree
  OCTA: wake of middle vertex
  Kagome: top and bottom plates are different
  Kagome: in the wakes, but asymmetric

## Slide 40: Overall Nu and f Comparison
Pressure drop improvement: 45 degree rotation improved pressure drop by 25% - 32% in OCTA, 18% to 20% for FC, while only 3% to 7% for BC.
Heat transfer: At lower Re, upto 15% lower enhancement in FC, and 18% lower enhancement in OCTA. Not much effect on BC.
The efficiency factor varied from ~0.6 to ~1.2 and similar for all cases
OCTA
Kagome
Kagome

## Slide 41: Summary
Transpiration cooling
The AM transpiration cooling structures could provide significant improvement on cooling efficiency ( > 30%) compared to film cooling.
Mechanical strength of the AM transpiration wall was much higher than conventionally fabricated(compressing and sintering) porous wall.
The cooling effectiveness could be further improved by increasing the compactness of the structure(ratio of the internal air-metal interface area to the volume).
Lattice cooling
Lattices provided higher heat transfer compared to that of the baseline pin-fin bank.
The unit cell geometry as well as their orientation w.r.t. flow affected the heat transfer and pressure drop behavior. However, the pressure drop characteristics had a stronger dependency on the unit cell rotation or angle-of-attack than heat transfer.
Secondary flows with flow diversion induced primarily by unit cell nodes, provide a unique opportunity to tailor a favorable coolant re-distribution inside channel.