## Slide 1
Rare Earth Elements and Critical Minerals from Coal-Based Resources
Mary Anne Alvin
NETL Rare Earth Elements & Critical Minerals Technology Manager
August 18, 2020
ACS Fall 2020 Virtual Meeting and Expo
Critical Materials Symposium
Critical Materials: Perspectives from the Industry, Government and Research Communities

## Slide 2: REE-CM Program
Mission
Develop Economic, Competitive, Sustainable Domestic Supply
National and Economic Security
Objectives
Recovery from Coal-Based Resources
Advanced REE-CM Separation Systems
Drivers/Challenges
Off-Shore Supplier Dominance
Market Volatility & Potential Price Manipulation
Low REE-CM Content in Coal-Based Resources

## Slide 3: REE-CM Program Goals & Metrics
Goals
Validate Technical-Economic Production
Accelerate Domestic Prototype Facility Demonstration
Produce Commercial-Grade REO Mixed Concentrates & Beyond
Environmentally Benign Processing
Metrics
Production of 1-3 tonnes (MT)/day of Mixed REO/RES
Minimum REO/RES Concentration  75% by weight
U.S. Demand (2015)
11% of Annual Global REE Market
16,000 tonnes/yr (44 tonnes/day)

## Slide 4: REE-CM Program Structure

## Slide 5: REE-CM Program: NETL Extramural Projects
Bench-to-Pilot-Scale REE Separation Facilities
REE Separation-Recovery
Pilot-Scale REE Separation Facilities

## Slide 6: REE-CM Program: Bench-Scale Processing
Acid Mine Drainage (AMD)
July 2018 Commissioned Facility
100% REE Recovery
Production of ~98% Mixed REO
CM Recovery
Small AMD sludge drying cell
0.5 ac, 10 ft deep, 80% moisture
Sludge DW 1,300 ton
$190/ton of sludge DW
In situ REE value = $247,000
Courtesy of Paul Ziemkiewicz, WVU

## Slide 7: REE-CM Program: Bench-Scale Processing
Low-Rank Coals  Lignite
High Organic REE Association
One-Step Selective Mineral Acid Leaching Process
~43% REE Recovery
Production of ~65% Mixed REO
CM Recovery
Courtesy of Nolan Theaker, UND

## Slide 8: REE-CM Program: Modular Pilot-Scale Processing
Coal Refuse  Central Appalachian & Illinois Coal Basins
Initiated Operation in June 2018
Production of REE in October- November 2018
~98% Mixed REO Concentrate Produced
CM Recovery
Courtesy of Rick Honaker University of Kentucky Roe-Hoan Yoon Virginia Tech
Youtube video link: https://www.youtube.com/watch?v=jR70j-MzWNE

## Slide 9: REE-CM Program: Pilot-Scale Processing
Coal Ash from Eastern Kentucky
Coal Physical Processing Pilot:
0.4 tpd Operational  CAER
Micro-Pilot Plant: 0.5 kgpd  PSI
Chemical Processing Pilot: 0.5 tpd
Operational November 2019  Winner Water
Courtesy of Prakash Joshi & David Gamliel, PSI

## Slide 10: REE-CM Program: NETL Intramural Project
Field Prospectivity &
Materials Characterization
Real-Time Aqueous REE Detection
Fiber Optic Probe (10s ppb)
Miniaturized LIBs Prototype (1 ppm)
U.S. Coal Basin Sedimentary Assessment
National-Level Geological, Geochemical & Geospatial Assessment Database Development
REE-Enriched Powder River Basin (PRB) Core Materials (>2,000 ppm) Identified
REE Separation-Recovery & TEA Process Economics
Acid Mine Drainage Solids
Staged Leaching  Production of 95% REOs
Fly Ash
96% REO Production at 10% Normal Acid Consumption
NETL BIAS Sorbent
Production of 95% REE from Synthetic AMD
Field Testing Initiated March 2020
Central Appalachian Basin Underclays
Mild Acid Extraction Testing with BIAS Sorbent
Process Economics
TEA Cost Analysis Tool Developed
NETL Research & Innovation Center (RIC)

## Slide 11: REE-CM Program: Other National Lab R&D
Rapid Luminescent Sensing of Lanthanides in Fluoride Hosts (Coal Fly Ash Leachates)
Si Sol-Gel Microbial Media for 2-Stage Sc/Ln+Y Recovery from Coal- Based Leachates
Continuous Packed-Bed Bioreactor System for REE Capture
Materials Characterization & Monitoring
REE Separation & Recovery
Chemistry & Mineralogy of Coal-Based Resources
Raman-LIBS Back-Pack Instrumentation (Mars)
Technology Transfer of Actinide Separation to REE Lanthanide Recovery

## Slide 12: REE-CM FOAs Issued in FY19 and FY20
DE-FOA-0002003
Process Scale-Up and Optimization/Efficiency Improvements for Rare Earth Elements (REE) and Critical Materials (CM) Recovery from Coal-Based Resources
Issued: January 31, 2019
Awarded: September 30, 2019
Definitized: January 1, 2020
RFP-89243320RFE000032
Production of Mixed Rare Earth Oxides (REOs) from Coal-Based Resources
Issued: April 22, 2020

## Slide 13: REE-CM Program: Where We Are Today
Courtesy of Inventure Renewables
Diversity of Coal-Based Feedstocks
Fully Integrated Program  Basic Science (TRL 1-3) to Pilot Facilities (TRL 5 to 7)
Demonstrated Technical Feasibility of REE Recovery
Three Domestic, First-of-a-Kind, Separation Facilities
  Small Quantities of REEs Produced
Cobalt (Co) & Other CM Production Demonstrated
Pending Commercial-Scale Extraction Efficiency, Preliminary Estimates Indicate
  Potential Supply ~22 MT/day Nd/Pr from Combined Coal-Based Resources (~25% Permanent Magnet International Demand)

## Slide 14: REE-CM Program: Near-Term Next Steps
Program Direction
Demonstration-Scale Facility  Mixed REO Concentrates
Economic & Process Efficiency Improvements
Address Technology Gaps
Metalization
REE-CM Co-Production

## Slide 15: REE-CM Program: Acknowledgments
July 2018
Active and Inactive Projects
Wyonics, LLC
Anactisis, Inc.
DOE-FE Personnel, External Stakeholders, NETL TDIC Federal Project Managers, NETL RIC Scientists and Engineers

## Slide 16: REE-CM Program – Contact Information
Mary Anne Alvin
Rare Earth Elements & Critical Minerals Technology Manger
412.386.5498 | Maryanne.Alvin@netl.doe.gov
National Energy Technology Laboratory
Visit Us at:
http://www.netl.doe.gov/research/coal/rare-earth-elements/
https://edx.netl.doe.gov/ree/
Courtesy of NETL REE-CM Website