## Slide 1: Modular Processing of Flare Gas for Carbon Nano-products (CNPs)
DE-FE0031870
Investigators:
Alan Weimer (PI), University of Colorado Boulder
Mija Hubler (co-PI), University of Colorado Boulder
Arrelaine Dameron, VP, Forge Nano
Colin Lobo, VP, National Ready Mixed Concrete Association
Program Managers:
David Cercone, Project Manager, DOE/NETL
Jodi Collins, Contract Specialist, DOE/NETL
DOE/NETL Project Kickoff Meeting, WebEx, June 29, 2020

## Slide 2: Project Elements/Overview
Awarded under DOE DE-FOA-0002006 - AOI 2B - Modular Equipment and PI Design Concepts for Conversion of Flare Gas to High-Value Carbon Products
Interdisciplinary team between one university (two
departments), an industry partner, and an expert
product association
  University of Colorado Boulder (Lead)
  Forge Nano (industry subcontractor)
  National Ready Mixed Concrete Association (non-profit association subcontractor)
Three-year project started on May 1, 2020
Total project budget: $3,750,000 ($3,000,000 from DOE and $750,000 from the participants as costshare)

## Slide 3: Background
Natural Gas Flaring
  Natural gas production in the United States has risen dramatically due to the “shale boom” and wide implementation of hydraulic fracturing;
  With gas prices at historic lows, it is generally not cost effective to invest in expensive infrastructure to transport gas, resulting in increased flare volumes;
  According to the EIA, approximately 36% of natural gas extracted in 2012 in North Dakota did not make it to market, with 29% of that gas being flared; although flaring dropped in subsequent years preceding 2015, the percentage of gas flared in October, 2018 in North Dakota grew to 20 percent, the highest the state has seen since August 2015;
  This translates to about $1 billion in lost revenue, and greenhouse gas emissions equivalent to adding 1 million cars to the road.
Producers often exhaust tight oil wells rather quickly because production from a single well depletes rapidly.

## Slide 4: Daily Production Rate from a Typical Tight Well
~ 20X decrease in 1st 5 years
700 Mcf/d
30 Mcf/d
Mcf/day

## Slide 5: Proposed Profitable Alternative
Distributed NG de-carbonization to value-added product
  Chemical vapor deposition (CVD) to carbon nano-product (CNP)
  CNP (carbon powder and carbon nanofibers) is value-added concrete additive for infrastructure
  Sequesters carbon in concrete & decreases CO2 emissions
    CNP addition to concrete could double concrete lifetime
    Reduce CO2 emissions by 0.9 to 1.4 B kg CO2/yr
  Build mobile CVD reactors that can be deployed as needed
    Simple 1-step chemical process (CH4  CNP + 2H2)
    Use sacrificial catalyst, eliminating expensive separation to recycle the catalyst; burn resulting H2 with unreacted CH4 to supply heat needed to drive the reaction
Similar to commercial gas phase polymerization

## Slide 6: Proposed Process Schematic
CHEN
CVEN

## Slide 7: Proposed Process Schematic
CHEN
CVEN

## Slide 8: Proposed Process Schematic
Forge Nano
NRMCA
NewCo

## Slide 9: Proposed Process Schematic
Forge Nano
NRMCA
NewCo
CHEN
CVEN

## Slide 10: CVD Using a Sacrificial Catalyst
CH4  C + 2H2

## Slide 11: CVD Using a Sacrificial Catalyst
CH4  C + 2H2

## Slide 12: Active CVD Catalysts (Fe, Ni, Co)

## Slide 13: Complete R&D Effort of the Project

## Slide 14: Complete R&D Effort of the Project
Overall Objective: Develop a simple and low-cost, CVD, one-step,
modular/mobile process to grow CNPs on a sacrificial catalyst that
will improve the durability of concrete (achieve TRL 5)

## Slide 15: The Team
Alan Weimer (PI)
  Professor, Chemical Engineering, University of Colorado Boulder (CU)
  Particle ALD, fluidization, solids processing, high-temperature chemistry
    Kent Warren, Post Doctoral Associate
    Gage Sowell, Jessica Hauck (pending), GRAs
    Theodore Champ, Research Assistant
Mija Hubler (Co-PI)
  Asst. Professor, CVEN, CU
  Cementitious materials, microstructure design, fracture mechanics
    Linfei Li, Post Doctoral Associate (FN pending)
Arrelaine, Dameron
  R&D Director, Forge Nano (FN)
    Andy Broerman, Principle Engineer
Colin Lobo
  VP Engineering, National Ready Mixed Concrete Assocation (NRMCA)

## Slide 16: Roles, Responsibilities and Collaborations (Project Management)
Task 1: Project Management & Planning
Task 2: Particle ALD Catalysis and CVD Synthesis Range Finding
Task 3: Design and construction of modular process
Task 4: Cement Mix Design using Commercially Available CNPs
Task 5: Bulk Production of CNPs and Technology to Market
Task 6: Cement Mix Design using Produced CNPs
Weekly 1 hr Meetings (Mondays 1300-1400, MST)

## Slide 17: Pressurized CVD Lab Reactor System
Capable of operating up to 450 psig and 900oC
CNFs grow on the fluidized catalyst/silica fume particles
Inconel or high-temp SS reactor tube/components
Reaction progress measured by in-situ mass spectrometer/NDIR at outlet

## Slide 18: Experimental Plan
Design methods leveraged to reduce experiment plan complexity, while maximizing insight
Catalyst synthesis: metal, cycle number, reaction temperature
CVD/CNF Growth: Gas hourly space velocity of natural gas, operating pressure
Species | Mole Fraction (%)
CH4 | 52.7
C2H6 | 24.6
C3H8 | 12.9
C4H10 | 1.3
H2S | 3.8
CO2 | 2.8
N2 | 0.0
He | 0.4
Total | 98.5

## Slide 19: Particle ALD Catalyst
Adatom nanoparticles (Fe, Co, or Ni) uniformly deposited on silica fume via ALD…
  Maintain catalytic activity
  Remain stable, e.g., resist further oxidation upon exposure to air
  Promote efficient use of the metal/M-ocene precursors

## Slide 20: Envisioned Process Flow Diagram for R&D Skid
Electric furnace
Fluidized reactor
Gas Solid separation
Feed Gas
Mixing
Product gas to safe location
Gas Analysis
Fresh Catalyst
CNT Product

## Slide 21: Envisioned Industrial Mobile Skid
Natural Gas Feed
ALD Catalyst
Gas out
Lock Hopper
and Cooling
Agglomerator
And Storage
Product
Exhaust
Air
Heat
Optional Regenerative Burner
Reactor 700-900°C
Heat
ALD Catalyst Storage
ALD Catalyst Lock Hopper

## Slide 22: Ready Mixed Concrete
Concrete - most used construction material
US Consumption (2019)
  Cement – 100 M metric tons
  Concrete – 500 M cu. yds. (RMC = 370 M yd3)
Industry Value (USGS)
  Cement - $12.5B
  Concrete - $65B
Average Price
  Cement - $120 – 150 / t
  Concrete - $100 – 500 / yd3
Cement
Water
Sand
Stone
Air
Vol.
6%
18%
10%
25%
40%
Wt.
0%
10%
15%
30%
45%

## Slide 23: Ready Mixed Concrete
Concrete is versatile
  Design for varying strength, durability, aesthetics
  Strong, resilient, minimum maintenance
  Long service life – 20, 50, 100+ years
Cement manufacture attributed to 5% global CO2
  Calcination of limestone
  Burning fossil fuels
Concrete uses recycled materials to minimize cement use
  Ash from burning coal
  Slag from iron manufacture
  Other materials
Contributes to sustainable construction
  Design and structural efficiency
  Resilience, energy use, service life,
  End of life recycling

## Slide 24: Scientific Principles & Objectives for CNF Integration into Concrete
Identify optimal processing methods
Determine permeability mechanisms
Standard product testing
Determine cracking mechanisms
Establish governing-processing-performance relations

## Slide 25: Concrete Design

## Slide 26: TEA - Flare Gas Properties
Species | Mole Fraction (%)
CH4 | 52.7
C2H6 | 24.6
C3H8 | 12.9
C4H10 | 1.3
H2S | 3.8
CO2 | 2.8
N2 | 0.0
He | 0.4
Total | 98.5
Composition of Flare Gas Stream1
Planned Site Location: Bakken Region, North Dakota
Average Flare Volume, 2018: 27.4 MCF per day1
Inlet pressure: 500 psi (34.47 bar)
1 National Energy Technology Laboratory, personal correspondence
2 Wikimedia Commons, https://commons.wikimedia.org/w/index.php?curid=5667339
2

## Slide 27: TEA - Process Flow Diagram
900°C
34.2 bar
Air
23,800 scf hr -1
Mole Fractions
73% N2
9.1% O2
2.9% CO2
15% H2O
560°C
1,142 scf hr -1
Flare Gas Feed
Catalyst & Support
CNF
99.9% H2
16.8 kg hr -1
70% conv

## Slide 28: TEA - Process Simulation
Heat Streams (Negative is exothermic)
C1: -6950 cal/sec
C2: -1748 cal/sec
C3: -5509 cal/sec
C4: -42483 cal/sec
BURNER: -19922 cal/sec
CVDRXR: 75022.6 cal/sec

## Slide 29: Scope of Work
Three Budget Periods
Budget Period I (17 months): Build lab research reactor process & initiate Particle ALD catalyst/CVD process research, preliminary TEA, pilot skid designed & construction started, concrete studies with purchased CNPs
Budget Period II (12 months): Build pilot skid & start up, Test particle ALD mixed-metal catalysts & select preferred catalyst and operating conditions (T, GHSV, …), optimize cement mix design using purchased CNPs, TEA will be updated
Budget Period III (12 months): Optimize pilot skid performance and produce CNPs for in-house testing, optimize cement mix design using in-house produced CNPs, kinetics studies using preferred catalyst, finalize TEA and T2M

## Slide 30: Gantt Chart

## Slide 31: Deliverables (Tasks 2 to 6)
Task/ Subtask | Milestone Title & Description | Planned Completion Date | Verification method
2.1 | A: The Lab Particle ALD FBR reactor system is started up Go/No Go | End of Q6 | Minimum fluidization velocity determined for fumed silica at up to 900oC.
2.2 | B: CVD will be carried out | End of Q8 | The solid product will comprise at least 25 wt% as measured using LECO combustion analysis
3.1 | C: Complete plans for module construction | End of Q6 | Review by engineer leading construction
3.2 | D: Pilot skid is started up Go/No Go | End of Q10 | Production of carbon nanoproduct from associated gas at the prescribed scale
4.1 | E: Mix design including carbon products | End of Q4 | Minimal (< 3 min) reduction in set time and an improved ductility compared to the baseline mix.

## Slide 32: Deliverables (Tasks 2 to 6)
Task/ Subtask | Milestone Title & Description | Planned Completion Date | Verification method
4.2 | F: Optimal cement mix design parameters will be identified | End of Q6 | Meet UHPC performance metrics using commercially available carbon nanoparticles and CNFs.
5.1 | G: Mix design including produced carbon product from sacrificial adatom catalyst | End of Q13 | Minimal (< 3 min) reduction in set time and an improved ductility compared to the baseline mix.
6.2 | H: Cement mix design parameters will be identified for mixes that meet UHPC performance using carbon products synthesized from sacrificial adatom catalyst. End of Project (final report) | End of Q14 | Meet compressive strength, flowability, flexural strength, and hydration time of UHPC using synthesized carbon products.

## Slide 33: Success Criteria
Phase 1: Solid CNPs are synthesized using ALD processes in the lab;
Phase 2: A pilot modular unit designed by CU and Forge Nano, constructed at CU, and set up at Forge Nano for experimentation;
Phase 3: Cement cylinders containing the CNPs which meet or exceed UHPC performance metrics;
Phase 4: The pilot unit demonstrates methane decarbonization producing the CNPs in bulk (>1kg of carbon product) and meeting metrics prescribed in Task 5.
Final Project Success: A TRL=5 is achieved

## Slide 34: Risk Management
Perceived Risk | Risk Rating |  |  | Mitigation/Response Strategy
 | Probability | Impact | Overall | 
 | (Low, Med, High) |  |  | 
Technical/Scope Risks: |  |  |  | 
Performance of the catalyst | Med | Med | Med | Consider multiple catalysts simultaneously to discover the best performing one
Management, Planning, and Oversight Risks: |  |  |  | 
Hiring challenges for GRA or PRA | Low | High | Med | Initiate search immediately upon award and transition those already at CU
ES&H Risks: |  |  |  | 
Nanoparticle release | Low | High | Med | Agglomerate and disperse all carbon products in liquids

## Slide 35: Budget

## Slide 36
Questions?