## Slide 1
Enhancing Coking Tolerance and Stability of SOFC Anodes Using ALD of Oxide Thin Films
Raymond J. Gorte, John M. Vohs
University of Pennsylvania
and
Steve McIntosh
Lehigh University

## Slide 2
Anode Issues:
Hydrocarbon tolerance 2) Sulfur tolerance
Ni-YSZ Anode – 1273 K
H2 + x ppm H2S
From Matsuzaki and Yasuda, Solid State Ionics, 132 (2000) 261.

## Slide 3
Anode Issues:
3) Poor redox stability
Ni oxidation by O2 or high H2O:C ratios causes fracture of the anode.

## Slide 4
“Engineer” the surface composition of the anode to introduce barrier layer.
Determine the effect of oxide coatings on electrode performance.
Goals
Technical Approach
Use atomic layer deposition (ALD) to selectively deposit oxide thin films onto both cathodes and anodes.
Determine the effect of films on electrode performance.
Program Goals and Approaches:

## Slide 5
Idea: Grow CaTiO3 on top of Ni cermet
30-wt% CaTiO3 on MgAl2O4:
ACS Catal., 8 (2018) 7679.

## Slide 6
Ni/CaTiO3/MgAl2O4 exposed to 10% CH4-He at 800 °C for 12 h
ACS Catal., 8 (2018) 7679.
CaTiO3 suppresses carbon formation for Ni

## Slide 7
Atomic Layer Deposition (ALD)
Allows layer-by-layer control
Can deposit mixed oxides, including perovsites
Only surface composition is modified.

## Slide 8
Growth rates:
1) Can be measured gravimetrically
1-nm of CeO2 on 10 m2/g support is ~7-wt%
2) Similar for different oxides:
~1x1018 metal atoms/m2-cycle ~ 0.02-nm/cycle
3) 10 ALD cycles ~ 1 monolayer.

## Slide 9
1) ALD forms uniform films (not particles).
2) ALD does not change the surface area.
3) ALD allows formation of mixed-oxide, thin films.
Why ALD and not simple infiltration?
XRD of 1.0-nm, ALD films of ATiO3 on MgAl2O4
STEM of CaTiO3 on MgAl2O4

## Slide 10
High Sensitivity-Low Energy Ion Scattering:
LEIS
HS-LEIS
Large acceptance angle ( 360o )
Parallel Energy Detection

## Slide 11
Confirmation of Film Uniformity:
LSF cathode with:
0 cycles of Co
10 cycles of Co
40 cycles of Co
LEIS
XPS

## Slide 12
Depth Profiling of ALD by HS-LEIS
Fe deposition onto porous Al2O3 substrates.
Sub-monolayer coverage after 10 ALD cycles largely removed by three sputtering cycles
Full coverage after 20 ALD cycles.

## Slide 13
ALD Considerations:
Ni will rapidly if oxidized at high Temperatures
But to deposit metal oxides by ALD requires an oxidation step (400-500 °C in air)
Temperatures need to be lowered to prevent Ni oxidation
More reactive precursors are unstable
Stronger oxidants to lower oxidation T?
Ozone & O2 Plasma unable to oxidize precursors in porous materials
H2O2 comparable to oxygen for precursors of interest.
NO2: Strong oxidant but forms nitrates that need to be removed by a reduction step

## Slide 14
Demonstration of Precursor Oxidation by NO2:
1 g of (120 m2/g) y-alumina with 1 cycle of Ce-THMD precursor deposited
NO2 is pulsed in at 300 °C (detected as NO & NO2) , CO2 and CO are measured
300 °C
500 °C
O2
He
NO2 exposures

## Slide 15
Metal Nitrate reduction:
0.5 g of y-alumina with 1 cycles of Ce-THMD precursor deposited
Sample is exposed to NO2
TPR is performed in H2 to enhance metal-nitrate decomposition
Evolution of NOx species is clear with trace amounts of H2O

## Slide 16
Ce(TMHD)4 -NO2-H2 ALD was performed on 120 and the weight gain was studied to determine the growth rate (Deposition T: 230 °C, Oxidation & Reduction T: 300 °C)
(
Average of 1.17 % wt change/cycle
Proposed reactions:
Confirmation of Ce ALD growth rate:

## Slide 17
Test for Enhanced Coke Tolerance in Ni-YSZ by CeO2 ALD.
Methods:
Ball mill NiO:YSZ+C powders (60:40, 10 wt%)
Press into slabs
Sinter at 1450 °C for 4 hours, and reduce at 700 °C for 2 hours
Deposit Ceria with ALD
Coking Test: Expose to dry CH4 (25ml/min) at 750°C for 2 hours

## Slide 18
Metal surface is unstable during deposition
Large carbon deposits with or without Ceria
NiO film at RT, expands during ALD (300 °C oxidation)
Upon re-reduction the microstructure change disrupts the ALD film
Metal oxide ALD is not practical for creating continuous films on Ni cermets unless it can be performed at very low temperatures
Metal ALD (under reducing conditions) is more likely to succeed

## Slide 19
Isopropanol TPD
20 wt% Ni/ZrO2
20 Ceria ALD/Ni/ZrO2
15 wt% Ceria infiltration +
20 wt% Ni/ZrO2
20 Ceria ALD/Ni/ZrO2
Then 2 hr re-reduction at 700 °C
Ni surface
Ceria coated surface
Ni-Ceria surface
Ni-Ceria surface
Ni is exposed! HC Cracking will occur
Surface chemistry is changed, but microstructure is unstable

## Slide 20
Enhancing Coking Tolerance and Stability of SOFC Anodes Using ALD of Oxide Thin Films
Raymond J. Gorte, John M. Vohs
University of Pennsylvania
and
Steve McIntosh
Lehigh University