## Slide 1: A Transformational Natural Gas Fueled Dynamic SOFC for Critical Datacenter In-Rack Power
DE-FE-0031671
University of South Carolina
PI: Prof. Kevin Huang
Co-PI: Prof. Frank Chen
Project Period: August 17, 2018 – August 16, 2020
2020 Annual SOFC Review Meeting
July 10, 2020

## Slide 2: Project Objective
To develop robust metal-bed compositions for new datacenter-suitable dynamic NG-fueled SOFC system

## Slide 3: Project Status
Tasks | Deliverables | Status
Optimizing active metal/oxide ratio | Metal/oxide ratio (wt%): 90:10 | Complete
New metal phase compositions/segmented bed | Fe-30mol%Ni | Complete
New sintering-resistant and active oxide support | BaCe0.7Zr0.1Y0.1Yb0.1O3 | Complete
Sintering-resistant active metal particles | Fe2O3@SiO2 core-shell | Complete
SF-bed testing in SOFC | N/A | Ongoing

## Slide 4: Outline
Results
  New metal-bed compositions: Fe-Mn and Fe-Ni systems
  New metal-support composition: BaCe0.7Zr0.1Y0.1Yb0.1O3-
  New Fe2O3@SiO2 redox stable core-shell structure
  TPR study
  Chemical looping study
  Mechanism for improved redox stability by Fe-Ni alloy
Summary
Ongoing activities
Acknowledgement

## Slide 5: Metal-Bed Phase Composition Change during Redox Cycle
Reduction
Reduction
Fe-Mn system
Fe-Ni system
(Fe2O3-Mn2O3)s-ZrO2
(Fe-Mn)s-ZrO2
(Fe-Ni)s-ZrO2
(Fe2O3-NiO-NiFe2O4)-ZrO2

## Slide 6: TPR Profiles
Fe-Mn system
Fe-Ni system
Mn-addition slows down reduction
Ni-addition accelerates reduction

## Slide 7: TPR of Fe-bed with Different Oxide Supports
10oC/min
Proton containing BCZYYb (BaCe0.7Zr0.1Y0.1Yb0.1O3) is the best to facilitate the reduction of Fe2O3

## Slide 8: Chemical Looping Hydrogen (CLH) System
Water syringe pump
Mass flow controller
4-way switch
PLC controller
CLH reactor
MS
Connect to MS

## Slide 9: Calibration of MS
Integration of signal

## Slide 10: Calculation of Hydrogen Production and Consumption
10%H2-Ar
10%H2O-Ar
(10 sccm H2)
The volume of H2 yield = ;
The volume of H2 consumption = ;
is the area of H2 production (oxidation peak);
is the area of total input hydrogen (rectangle);
is the area of reduction peak, so the consumption of hydrogen during reduction corresponds to the .

## Slide 11: CLH – Baseline Fe-ZrO2
Reduction
No significant morphology change
Before CLH
After CLH

## Slide 12: CLH – Fe-Foam
Pure Fe-foam
Pure Fe-YSZ foam
Significant morphology change
Before CLH
After CLH
After CLH
Moderate morphology change
Before CLH
After CLH
After CLH
Reduction
Reduction

## Slide 13: Comparison between Baseline and Fe-Foam
Severe sintering and low surface area in Fe-foam led to fast performance decade

## Slide 14: CLH – Fe-Ni Foam
Fe-Ni foam is more stable than Fe-foam during CLH, but has lower H2 production rate

## Slide 15: CLH – Fe-Ni-ZrO2 (powder)
Testing condition: 10% H2 and Argon, oxidation of 5 min and reduction of 15 min; 0.21g oxygen carrier materials.
The hydrogen yield was defined as the accumulated volume of hydrogen (mL g-1) produced during oxidation process divided by the mass of active materials and the hydrogen production rate (mL g-1 s-1) is hydrogen yield divided by the oxidation- ycle time (5 min).
No ZrO2 added

## Slide 16: CLH – Fe-Ni-ZrO2
5wt% ZrO2 added
10wt% ZrO2 added

## Slide 17: CLH – Fe-Ni-ZrO2
15wt% ZrO2 added
20wt% ZrO2 added

## Slide 18: Comparison of H2 Production by Fe-Ni-ZrO2
From testing results, the Fe-Ni 7:3 (mol%) doped 20wt% Zr shows the highest hydrogen yield (~300 mL g-1 after 40 cycles) and the best cycling stability with the redox efficiency of ~100%.

## Slide 19: Fe-Ni-O Phase Diagram
O, at%
O (1/2O2)
Fe
Ni
FeO
Fe3O4
Fe2O3
NiO
0.30Ni
NiFe2O4
Fe, at%
Ni, at%
Equilibrium triangles:
 (Fe-Ni)-FeO
 FeO-Fe3O4-NiO
 Fe3O4-NiO-NiFe2O4
 Fe3O4-Fe2O3-NiFe2O4
 Fe2O3-NiFe2O4-O2





Adding O (oxidation)
XRD results are consistent with phase diagram prediction in phase composition during the oxidation cycle

## Slide 20: Mechanisms of Improved Fe-Ni Redox Cycle
In Pure Fe, the redox cycle causes a net outward Fe diffusion due to “Kirkendall” effect, leading to irreversible growth of internal micro-porosity in Fe body and formation of a dense, gas-blocking shell at the exterior surface
In Fe-Ni alloy, during oxidation it transforms into a composite structure with a Ni-rich alloy core and oxide surfaces. The internal Ni-rich phase imparts mechanical integrity against oxide fracture and spallation
During reduction, the Ni-rich phase maintains adhesion to the FeO/Fe3O4 surfaces, and Ni catalyzes Fe reduction at the metal/oxide interface, at which Fe diffuses inward to the Ni-rich core and Fe-Ni re-homogenization eliminates the micro-porosity formation during oxidation
Fe-30Ni

## Slide 21: Fe2O3@SiO2 Core-shell
Sintering at 600oC for 5h
100 nm Fe2O3

## Slide 22: CLH - Fe2O3@SiO2 Core-shell
The performance is comparable to Fe-30Ni-20wt%ZrO2

## Slide 23: Conclusions
Fe-30mol%Ni alloys is a better choice for solid-fuel composition than pure Fe due to its better resistance to “Kirkendall” effect
Chemical looping studies confirm that Fe-30mol%Ni with 20wt% ZrO2 has the highest and most stable H2 production rate
BaCe0.7Zr0.1Y0.1Yb0.1O3 (BCZYYb) is a better oxide than ZrO2 for active metal support due to its high proton concentration
A promising Fe2O3@SiO2 composition is identified as a potential metal-bed composition
18

## Slide 24: Ongoing Activities
Continuing CLH testing on Fe2O3@SiO2
Tubular cell making
Testing Fe-Ni-ZrO2 bed with BCZYYb support
18
Furnace
MFC
TC
Bubbler
EC station
Computer
Ventilation

## Slide 25: Acknowledgement
DOE NETL for supporting this work under award DE-FE-0031671
Diane Revay Madden is the project manager and Dr. Shailesh Vora is the program director